# AUTOTEX F200 POLYESTER

Face:

High quality textured polyester film. For applications requiring a combination of high abrasion resistance and flexibility. Resistant to alcohols, dilute acids & alkalis, esters, hydrocarbons, ketone and household cleaning agents.

Thickness:                 200micron ±5%

Temp Range:                        -40ºC to +85ºC

Min. Application Temp:      -40ºC